## Slide 1
Micromechanics: Computational Cell
Array of voids
Computational cell
Void volume fraction
Finite element model
Ductile fracture
Microstructure idealization
Modeling idealization
Void elongation ratio
| 7 |

## Slide 2
Micromechanics: Stress State
Macroscopic stresses:
are area averages
Triaxiality:
Lode parameter:
third invariant of deviatoric stress
Hydrostatic stress; Von-Mises stress
The influence of Lode parameter is negletted in this study – it is not possible to obtain a wide range of Lode parameters when working with sheet metal

## Slide 3
Void Dilation Equations
Chart: Macroscopic strain
Chart: Macroscopic strain
 | Void dilation evolution
0.25 | 
0.50 | 
0.75 | 
1.00 | 
1.25 | 
1.50 | 
0.25 | 
0.50 | 
0.75 | 
1.00 | 
1.25 | 
1.50 | 
 | Void dilation evolution
0.25 | 
0.50 | 
0.75 | 
1.00 | 
1.25 | 
1.50 | 
0.25 | 
0.50 | 
0.75 | 
1.00 | 
1.25 | 
1.50 | 
Ferrite
Chart: Macroscopic strain
 | 0.0098575 | 0.0098703 | 0.0098831 | 0.0098965 | 0.0099132 | 0.0099354 | 0.0099746 | 0.01003 | 0.010106 | 0.010221 | 0.010408 | 0.010714 | 0.01111 | 0.011535 | 0.01197 | 0.012411 | 0.012855 | 0.013304 | 0.013756 | 0.014217 | 0.014669 | 0.015128 | 0.015593 | 0.016069 | 0.016531 | 0.017013 | 0.017493 | 0.017971 | 0.018454 | 0.018948 | 0.019448 | 0.019941 | 0.020436 | 0.020942 | 0.021454 | 0.021968 | 0.022488 | 0.023011 | 0.02354 | 0.024074 | 0.024612 | 0.025157 | 0.025705 | 0.026258 | 0.026817 | 0.027381 | 0.027951 | 0.028526 | 0.03 | 0.035
Chart: Macroscopic strain
 | 0.0098575 | 0.0098703 | 0.0098831 | 0.0098965 | 0.0099132 | 0.0099354 | 0.0099746 | 0.01003 | 0.010106 | 0.010221 | 0.010408 | 0.010714 | 0.01111 | 0.011535 | 0.01197 | 0.012411 | 0.012855 | 0.013304 | 0.013756 | 0.014217 | 0.014669 | 0.015128 | 0.015593 | 0.016069 | 0.016531 | 0.017013 | 0.017493 | 0.017971 | 0.018454 | 0.018948 | 0.019448 | 0.019941 | 0.020436 | 0.020942 | 0.021454 | 0.021968 | 0.022488 | 0.023011 | 0.02354 | 0.024074 | 0.024612 | 0.025157 | 0.025705 | 0.026258 | 0.026817 | 0.027381 | 0.027951 | 0.028526 | 0.03 | 0.035
Martensite

## Slide 4
Void Dilation Equations[Contd.]
Chart: Triaxiality
| 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5
 | 0.4329 | 0.8996 | 1.6829 | 2.6087 | 3.806 | 5.657
Chart: Triaxiality
| 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5
 | 0.5606 | 1.1237 | 2.358 | 4.0127 | 6.3891 | 8.5112
where
Void dilation equation: Ferrite
Void dilation equation: Martensite
where
Ferrite
Martensite

## Slide 5
Martensite
Chart: Strain
| 0 | 1.0300000000000001E-3 | 2.0699999999999998E-3 | 5.5999999999999999E-3 | 1.15E-2 | 1.8599999999999998E-2 | 2.6200000000000001E-2 | 3.3700000000000001E-2 | 4.1200000000000001E-2 | 4.87E-2 | 5.6099999999999997E-2 | 6.3500000000000001E-2 | 7.0800000000000002E-2 | 7.8100000000000003E-2 | 8.5300000000000001E-2 | 9.2499999999999999E-2 | 9.9599999999999994E-2 | 0.107 | 0.114 | 0.121 | 0.128 | 0.13500000000000001 | 0.14099999999999999 | 0.14799999999999999 | 0.155 | 0.16200000000000001 | 0.16800000000000001 | 0.17499999999999999 | 0.182 | 0.188 | 0.19500000000000001 | 0.20100000000000001
 | 1 | 1.0029 | 1.0058 | 1.0163 | 1.0329 | 1.0535 | 1.0754 | 1.0975 | 1.1197 | 1.142 | 1.1643 | 1.1866 | 1.2089 | 1.2313 | 1.2537 | 1.2762 | 1.2987 | 1.3212 | 1.3438 | 1.3664 | 1.389 | 1.4117 | 1.4345 | 1.4573 | 1.4801 | 1.503 | 1.5259 | 1.5489 | 1.5719 | 1.5951 | 1.6182 | 1.6414
 | 1 | 1.0023 | 1.0046 | 1.0087 | 1.0199 | 1.0358 | 1.0549 | 1.075 | 1.0953 | 1.1156 | 1.1359 | 1.1562 | 1.1765 | 1.1968 | 1.2172 | 1.2375 | 1.2578 | 1.2781 | 1.2984 | 1.3187 | 1.339 | 1.3593 | 1.3795 | 1.3998 | 1.4201 | 1.4404 | 1.4607 | 1.481 | 1.5013 | 1.5216 | 1.5419 | 1.5622 | 1.5825
 | 1 | 1.0019 | 1.0038 | 1.0056 | 1.0117 | 1.0221 | 1.0365 | 1.0533 | 1.0708 | 1.0886 | 1.1064 | 1.1243 | 1.1422 | 1.1601 | 1.178 | 1.1958 | 1.2137 | 1.2315 | 1.2492 | 1.267 | 1.2847 | 1.3023 | 1.3199 | 1.3375 | 1.355 | 1.3725 | 1.39 | 1.4074 | 1.4247 | 1.4421 | 1.4594 | 1.4767 | 1.4939 | 1.5111
 | 1 | 1.0016 | 1.0033 | 1.0047 | 1.0067 | 1.0132 | 1.0221 | 1.0341 | 1.0479 | 1.0624 | 1.0772 | 1.0922 | 1.1074 | 1.1226 | 1.1378 | 1.153 | 1.1683 | 1.1834 | 1.1986 | 1.2137 | 1.229 | 1.2438 | 1.2588 | 1.2737 | 1.2885 | 1.3033 | 1.318 | 1.3325 | 1.3471 | 1.3616 | 1.376 | 1.3904 | 1.4046 | 1.4188 | 1.4329
 | 1 | 1.0014 | 1.0029 | 1.0041 | 1.005 | 1.0078 | 1.0125 | 1.0191 | 1.0278 | 1.0381 | 1.0492 | 1.0609 | 1.0729 | 1.0851 | 1.0975 | 1.1101 | 1.1225 | 1.1351 | 1.1476 | 1.1602 | 1.1729 | 1.1854 | 1.1976 | 1.2098 | 1.2222 | 1.2343 | 1.2464 | 1.2583 | 1.2702 | 1.282 | 1.2937 | 1.3054 | 1.3168 | 1.3282
 | 1 | 1.0013 | 1.0025 | 1.0036 | 1.0043 | 1.0046 | 1.0067 | 1.0088 | 1.0119 | 1.0168 | 1.0234 | 1.0311 | 1.0395 | 1.0487 | 1.0582 | 1.068 | 1.0778 | 1.0878 | 1.0977 | 1.108 | 1.118 | 1.1282 | 1.1382 | 1.148 | 1.1579 | 1.1678 | 1.1776 | 1.1873 | 1.1969 | 1.2066 | 1.2159 | 1.2252 | 1.2344 | 1.2435 | 1.2525 | 1.2614 | 1.2701
Chart: Strain
| 0 | 1.0300000000000001E-3 | 2.0699999999999998E-3 | 5.5999999999999999E-3 | 1.15E-2 | 1.8599999999999998E-2 | 2.6200000000000001E-2 | 3.3700000000000001E-2 | 4.1200000000000001E-2 | 4.87E-2 | 5.6099999999999997E-2 | 6.3500000000000001E-2 | 7.0800000000000002E-2 | 7.8100000000000003E-2 | 8.5300000000000001E-2 | 9.2499999999999999E-2 | 9.9599999999999994E-2 | 0.107 | 0.114 | 0.121 | 0.128 | 0.13500000000000001 | 0.14099999999999999 | 0.14799999999999999 | 0.155 | 0.16200000000000001 | 0.16800000000000001 | 0.17499999999999999 | 0.182 | 0.188 | 0.19500000000000001 | 0.20100000000000001
 | 1 | 1.0029 | 1.0058 | 1.0163 | 1.0329 | 1.0535 | 1.0754 | 1.0975 | 1.1197 | 1.142 | 1.1643 | 1.1866 | 1.2089 | 1.2313 | 1.2537 | 1.2762 | 1.2987 | 1.3212 | 1.3438 | 1.3664 | 1.389 | 1.4117 | 1.4345 | 1.4573 | 1.4801 | 1.503 | 1.5259 | 1.5489 | 1.5719 | 1.5951 | 1.6182 | 1.6414
 | 1 | 1.0023 | 1.0046 | 1.0087 | 1.0199 | 1.0358 | 1.0549 | 1.075 | 1.0953 | 1.1156 | 1.1359 | 1.1562 | 1.1765 | 1.1968 | 1.2172 | 1.2375 | 1.2578 | 1.2781 | 1.2984 | 1.3187 | 1.339 | 1.3593 | 1.3795 | 1.3998 | 1.4201 | 1.4404 | 1.4607 | 1.481 | 1.5013 | 1.5216 | 1.5419 | 1.5622 | 1.5825
 | 1 | 1.0019 | 1.0038 | 1.0056 | 1.0117 | 1.0221 | 1.0365 | 1.0533 | 1.0708 | 1.0886 | 1.1064 | 1.1243 | 1.1422 | 1.1601 | 1.178 | 1.1958 | 1.2137 | 1.2315 | 1.2492 | 1.267 | 1.2847 | 1.3023 | 1.3199 | 1.3375 | 1.355 | 1.3725 | 1.39 | 1.4074 | 1.4247 | 1.4421 | 1.4594 | 1.4767 | 1.4939 | 1.5111
 | 1 | 1.0016 | 1.0033 | 1.0047 | 1.0067 | 1.0132 | 1.0221 | 1.0341 | 1.0479 | 1.0624 | 1.0772 | 1.0922 | 1.1074 | 1.1226 | 1.1378 | 1.153 | 1.1683 | 1.1834 | 1.1986 | 1.2137 | 1.229 | 1.2438 | 1.2588 | 1.2737 | 1.2885 | 1.3033 | 1.318 | 1.3325 | 1.3471 | 1.3616 | 1.376 | 1.3904 | 1.4046 | 1.4188 | 1.4329
 | 1 | 1.0014 | 1.0029 | 1.0041 | 1.005 | 1.0078 | 1.0125 | 1.0191 | 1.0278 | 1.0381 | 1.0492 | 1.0609 | 1.0729 | 1.0851 | 1.0975 | 1.1101 | 1.1225 | 1.1351 | 1.1476 | 1.1602 | 1.1729 | 1.1854 | 1.1976 | 1.2098 | 1.2222 | 1.2343 | 1.2464 | 1.2583 | 1.2702 | 1.282 | 1.2937 | 1.3054 | 1.3168 | 1.3282
 | 1 | 1.0013 | 1.0025 | 1.0036 | 1.0043 | 1.0046 | 1.0067 | 1.0088 | 1.0119 | 1.0168 | 1.0234 | 1.0311 | 1.0395 | 1.0487 | 1.0582 | 1.068 | 1.0778 | 1.0878 | 1.0977 | 1.108 | 1.118 | 1.1282 | 1.1382 | 1.148 | 1.1579 | 1.1678 | 1.1776 | 1.1873 | 1.1969 | 1.2066 | 1.2159 | 1.2252 | 1.2344 | 1.2435 | 1.2525 | 1.2614 | 1.2701
Void Elongation Equations
Chart: Strain
| 0 | 1.0300000000000001E-3 | 2.0699999999999998E-3 | 3.1099999999999999E-3 | 5.2700000000000004E-3 | 8.2699999999999996E-3 | 1.2500000000000001E-2 | 1.8800000000000001E-2 | 2.64E-2 | 3.4200000000000001E-2 | 4.2099999999999999E-2 | 4.99E-2 | 5.7599999999999998E-2 | 6.5299999999999997E-2 | 7.2900000000000006E-2 | 8.0500000000000002E-2 | 8.7900000000000006E-2 | 9.5399999999999999E-2 | 0.10299999999999999 | 0.11 | 0.11700000000000001 | 0.125 | 0.13200000000000001 | 0.13900000000000001 | 0.14599999999999999 | 0.153 | 0.16 | 0.16700000000000001 | 0.17399999999999999 | 0.18099999999999999 | 0.187 | 0.19400000000000001 | 0.20100000000000001
 | 1 | 1.0029 | 1.0058 | 1.0087 | 1.0152 | 1.0236 | 1.0358 | 1.0541 | 1.0764 | 1.0998 | 1.1234 | 1.1472 | 1.171 | 1.1949 | 1.2189 | 1.243 | 1.2671 | 1.2914 | 1.3157 | 1.3401 | 1.3646 | 1.3892 | 1.4138 | 1.4385 | 1.4633 | 1.4882 | 1.5131 | 1.5381 | 1.5632 | 1.5884 | 1.6136 | 1.6389 | 1.6643
 | 1 | 1.0023 | 1.0046 | 1.0069 | 1.0096 | 1.0151 | 1.0218 | 1.031 | 1.0451 | 1.0643 | 1.0853 | 1.1066 | 1.1279 | 1.1492 | 1.1705 | 1.1919 | 1.2132 | 1.2345 | 1.2558 | 1.2771 | 1.2984 | 1.3197 | 1.341 | 1.3623 | 1.3836 | 1.4048 | 1.4261 | 1.4473 | 1.4686 | 1.4898 | 1.511 | 1.5322 | 1.5535 | 1.5747 | 1.5958
 | 1 | 1.0019 | 1.0038 | 1.0057 | 1.0076 | 1.0103 | 1.0148 | 1.0199 | 1.0266 | 1.0366 | 1.0513 | 1.0686 | 1.0864 | 1.1042 | 1.1219 | 1.1396 | 1.1573 | 1.1749 | 1.1924 | 1.2098 | 1.2271 | 1.2445 | 1.2617 | 1.2788 | 1.2959 | 1.3129 | 1.3298 | 1.3467 | 1.3633 | 1.3802 | 1.3965 | 1.4131 | 1.4295 | 1.4458 | 1.4622 | 1.4783
 | 1 | 1.0016 | 1.0033 | 1.0049 | 1.0065 | 1.008 | 1.0105 | 1.014 | 1.0178 | 1.0223 | 1.0286 | 1.0382 | 1.0504 | 1.0633 | 1.0764 | 1.0894 | 1.1024 | 1.1154 | 1.1284 | 1.1416 | 1.1542 | 1.1669 | 1.1795 | 1.1923 | 1.2044 | 1.2169 | 1.2291 | 1.241 | 1.2529 | 1.2648 | 1.2766 | 1.2879 | 1.2992 | 1.3104 | 1.3215 | 1.3325 | 1.3433
 | 1 | 1.0014 | 1.0029 | 1.0043 | 1.0056 | 1.0069 | 1.0081 | 1.0103 | 1.0128 | 1.0152 | 1.0176 | 1.0204 | 1.0246 | 1.0306 | 1.0374 | 1.0447 | 1.0523 | 1.0603 | 1.068 | 1.0761 | 1.0841 | 1.0921 | 1.1001 | 1.108 | 1.1159 | 1.1236 | 1.1314 | 1.1388 | 1.1464 | 1.1538 | 1.1609 | 1.1679 | 1.1747 | 1.1814 | 1.1877 | 1.194 | 1.2001
 | 1 | 1.0013 | 1.0026 | 1.0038 | 1.005 | 1.0061 | 1.007 | 1.0079 | 1.0095 | 1.0109 | 1.0118 | 1.0121 | 1.0115 | 1.01 | 1.0087 | 1.0085 | 1.0092 | 1.0107 | 1.013 | 1.0158 | 1.019 | 1.0225 | 1.0262 | 1.0301 | 1.0341 | 1.0382 | 1.0421 | 1.0461 | 1.0499 | 1.0536 | 1.0572
Ferrite
- Proportionality constant
1) Micro void elongation is prominent at low triaxialities for both ferrite and martensite
2) The void in ferrite tend to elongate rapidly when compared to the void in martensite for a given macroscopic strain at high triaxialities
3) The evolution of void elongation ratio is almost linear (similar to the evolution of void dilation) with respect to the macroscopic strain

## Slide 6
Chart: Triaxiality
| 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5
0.25 0.5 0.75 1 1.25 1.5 | 3.1647 | 2.877 | 2.531 | 2.1489 | 1.7444 | 1.3587
Ferrite
Chart: Triaxiality
| 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5
 | 3.2698 | 2.8722 | 2.3377 | 1.6989 | 1.0248 | 0.3176
Martensite
Void Elongation Equations[Contd.]
Evaluating proportionality functions
The proportionality functions are obtained by plotting slopes of void elongation evolution curves with respect to the triaxialities at which they are obtained

## Slide 7
Microscopic Damage Mechanisms
undeformed cell
deformed cell
dilated void
initial void
elongated void
initial void
Void Dilation
Void Elongation
Coalescence of dilated voids
Coalescence of elongated voids

## Slide 8
Modified LeMaitre Model
Stress rate and elastic strain rate
- elastic moduli of un-damaged material
Isotropic visco-plastic constitutive equation
Damage evolution equation
, are void coalescence parameters
critical damage parameter
critical void elongation ratio
Void elongation evolution
, are void elongation parameters

## Slide 9
Modified LeMaitre Model: Features
Features
1) The model accounts for the damage due to microvoid dilation and elongation based on damage evolution equations derived from micromechanical analysis
2) While the microvoid dilation can cause gradual local softening, microvoid elongation is assumed to cause damage only when the critical void elongation ratio is exceeded
3) The model can be used to identify the actual damage mechanism (microvoid dilation/ elongation) that ultimately initiates fracture
Limitations
1) The model does not account for the local anisotropy induced by microvoid elongation
2) The influence of microvoid rotation is ignored.

## Slide 10
Q&P980 Fracture Tests
Aim: to understand the influence of triaxiality on fracture strains of Q&P980 steels and thereby use this information for calibrating and
average triaxiality in the critical cross-section (least cross-sectional area)
Pure Shear 1
Shear
Tension
U-notch
Circular
Notched
Pure Shear 2
Specimens used for calibration of MLM

## Slide 11
Load Displacement Curves
Displacement rate – 0.02 mm/sec; DIC is use to acquire strain data (5 fps)
Three tests for each geometry are tested
Good repeatability of load displacement behavior and fracture strains are obtained

## Slide 12
MLM Calibration
C – Notch
Used for calibrating
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 0 | 0 | 3.3295900000000002E-4 | 1.1779399999999999E-3 | 2.27764E-3 | 3.9825900000000003E-3 | 7.5578399999999997E-3 | 1.59078E-2 | 2.8375399999999999E-2 | 4.1773999999999999E-2 | 5.5585900000000001E-2 | 7.0088999999999999E-2 | 8.53019E-2 | 0.10122100000000001 | 0.11801499999999999 | 0.135689 | 0.15429399999999999 | 0.173794 | 0.19440199999999999 | 0.216443 | 0.239231 | 0.262573 | 0.28568399999999999 | 0.30929400000000001 | 0.33297700000000002 | 0.35610700000000001 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998
 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005
 | 0 | 0 | 0 | 0 | 0 | 0 | 4.6119e-06 | 1.6519e-05 | 3.2463e-05 | 5.7787e-05 | 0.00011162 | 0.00023875 | 0.00042904 | 0.0006303 | 0.00083481 | 0.0010476 | 0.0012701 | 0.0015024 | 0.0017476 | 0.0020067 | 0.0022805 | 0.0025696 | 0.0028778 | 0.0032109 | 0.0035599 | 0.0039233 | 0.0042899 | 0.0046715 | 0.0050634 | 0.0055008 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 0 | 0 | 3.3295900000000002E-4 | 1.1779399999999999E-3 | 2.27764E-3 | 3.9825900000000003E-3 | 7.5578399999999997E-3 | 1.59078E-2 | 2.8375399999999999E-2 | 4.1773999999999999E-2 | 5.5585900000000001E-2 | 7.0088999999999999E-2 | 8.53019E-2 | 0.10122100000000001 | 0.11801499999999999 | 0.135689 | 0.15429399999999999 | 0.173794 | 0.19440199999999999 | 0.216443 | 0.239231 | 0.262573 | 0.28568399999999999 | 0.30929400000000001 | 0.33297700000000002 | 0.35610700000000001 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998
 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005
 | 0 | 0 | 0 | 0 | 0 | 0 | 4.6119e-06 | 1.6519e-05 | 3.2463e-05 | 5.7787e-05 | 0.00011162 | 0.00023875 | 0.00042904 | 0.0006303 | 0.00083481 | 0.0010476 | 0.0012701 | 0.0015024 | 0.0017476 | 0.0020067 | 0.0022805 | 0.0025696 | 0.0028778 | 0.0032109 | 0.0035599 | 0.0039233 | 0.0042899 | 0.0046715 | 0.0050634 | 0.0055008 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285
can be calibrated from a high triaxiality specimen
can be calibrated from a low triaxiality specimen
The model parameters that can accurately reproduce experimental load displacement curves are taken as calibrated MLM parameters
Chart: Displacement (mm)

 | 6.7126e-06 | 0.15555 | 0.62098 | 1.3927 | 2.4657 | 3.7898 | 5.0682 | 6.1364 | 6.9781 | 7.6493 | 8.1548 | 8.4574 | 8.6361 | 8.767 | 8.8708 | 8.9554 | 9.0239 | 9.0777 | 9.119 | 9.1484 | 9.167 | 9.1759 | 9.1741 | 9.1637 | 9.1448 | 9.1185 | 9.086 | 9.0473 | 9.0048 | -4.5315
C-Notch
Pure Shear – 1
Used for calibrating
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 7.1451000000000001E-4 | 3.1929699999999998E-3 | 7.9347099999999993E-3 | 1.55932E-2 | 2.6228100000000001E-2 | 3.9533800000000001E-2 | 5.4982400000000001E-2 | 7.2180300000000003E-2 | 9.0943599999999999E-2 | 0.11117200000000001 | 0.13273199999999999 | 0.15534999999999999 | 0.179066 | 0.203624 | 0.22862399999999999 | 0.25379000000000002 | 0.27950399999999997 | 0.30521700000000002 | 0.33053300000000002 | 0.354819 | 0.37886900000000001 | 0.401727 | 0.42452000000000001 | 0.44597300000000001 | 0.46659400000000001 | 0.48607899999999998 | 0.50420900000000002 | 0.52132999999999996 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003
 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7
 | 1 | 1 | 1 | 1.0029 | 1.0106 | 1.0252 | 1.0499 | 1.0841 | 1.1274 | 1.1777 | 1.2338 | 1.2949 | 1.3598 | 1.4284 | 1.5018 | 1.5761 | 1.6549 | 1.7349 | 1.8149 | 1.8949 | 1.9749 | 2.0549 | 2.1349 | 2.2149 | 2.2949 | 2.3655 | 2.4341 | 2.5027 | 2.5663 | 2.6234 | 2.6805 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007
Chart: Displacement (mm)
 | 9.7506e-05 | 0.10086 | 0.24685 | 0.47977 | 0.69813 | 0.87572 | 0.98 | 1.0287 | 1.1506 | 1.1772 | 1.2058 | 1.2311 | 1.257 | 1.286 | 1.316 | 1.3431 | 1.3614 | 1.4058 | 1.4416 | 1.4728 | 1.5094 | 1.5453 | 1.5792 | 1.6163 | 1.6535 | 1.6872 | 1.7529 | 1.7807 | 1.8081 | 1.794 | 1.4736 | 0.60725
MLM
Experiment

## Slide 13
Chart: Displacement (mm)

 | 6.7126e-06 | 0.15555 | 0.62098 | 1.3927 | 2.4657 | 3.7898 | 5.0682 | 6.1364 | 6.9781 | 7.6493 | 8.1548 | 8.4574 | 8.6361 | 8.767 | 8.8708 | 8.9554 | 9.0239 | 9.0777 | 9.119 | 9.1484 | 9.167 | 9.1759 | 9.1741 | 9.1637 | 9.1448 | 9.1185 | 9.086 | 9.0473 | 9.0048 | -4.5315
Chart: Displacement (mm)
 | 4.7254e-06 | 0.11618 | 0.45668 | 1.0229 | 1.8094 | 2.7994 | 3.9622 | 5.0512 | 5.9734 | 6.7348 | 7.3379 | 7.8557 | 8.2627 | 8.5478 | 8.7368 | 8.8737 | 8.9855 | 9.0809 | 9.1637 | 9.2355 | 9.2976 | 9.3514 | 9.3972 | 9.4356 | 9.4672 | 9.4934 | 9.5141 | 9.5298 | 9.5402 | 9.5456 | 9.5476 | 7.8368 | 6.2136 | 5.169 | 4.215 | 3.0367 | 0.87604 | 0.39128 | 0.36011 | 0.31131 | 0.13352
Chart: Displacement (mm)
 | 9.5749e-05 | 0.1992 | 0.5978 | 1.1961 | 1.7147 | 2.1215 | 2.3466 | 2.4613 | 2.5462 | 2.6207 | 2.6931 | 2.7632 | 2.8309 | 2.9013 | 2.9671 | 3.0333 | 3.098 | 3.1625 | 3.2264 | 3.2896 | 3.3499 | 3.4109 | 3.4698 | 3.5226 | 3.5757 | 3.6267 | 3.682 | 3.7256 | 3.7183 | 3.6493 | 3.6508 | 3.4784 | 0.89637 | 0.077112 | -0.29015 | 0.06659 | -0.0042944 | -0.25717 | -0.11217 | -0.040539 | -0.15873
Chart: Displacement (mm)
 | 9.7506e-05 | 0.10086 | 0.24685 | 0.47977 | 0.69813 | 0.87572 | 0.98 | 1.0287 | 1.1506 | 1.1772 | 1.2058 | 1.2311 | 1.257 | 1.286 | 1.316 | 1.3431 | 1.3614 | 1.4058 | 1.4416 | 1.4728 | 1.5094 | 1.5453 | 1.5792 | 1.6163 | 1.6535 | 1.6872 | 1.7529 | 1.7807 | 1.8081 | 1.794 | 1.4736 | 0.60725
Chart: Displacement (mm)
 | 5.2573e-05 | 0.136 | 0.40242 | 0.84917 | 1.4608 | 2.1016 | 2.6739 | 3.1495 | 3.4644 | 3.6357 | 3.7457 | 3.8332 | 3.9091 | 3.9766 | 4.04 | 4.0963 | 4.1483 | 4.1951 | 4.2368 | 4.2753 | 4.309 | 4.3398 | 4.367 | 4.3914 | 4.4107 | 4.4275 | 4.4411 | 4.447 | 4.4536 | 4.4556 | 4.46 | 4.455 | 4.4544 | 4.1944 | 1.4223
MLM: Load Displacement Prediction
MLM
Experiment
C-Notch
U-Notch
Pure Shear - 1
Pure Shear - 2
Shear Tension

## Slide 14
MLM: Fracture Initiation Locations
C-Notch
U-Notch
Pure Shear - 1
Pure Shear - 2
Shear Tension

## Slide 15
MLM: Microscopic Damage Mechanisms
Evolution of change in void volume fraction and void elongation ratio in critical finite element (the first element to fail) is plotted for all specimens
If ; coalescence of dilated voids
If ; coalescence of elongated voids
C – Notch
Used for calibrating
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 0 | 0 | 3.3295900000000002E-4 | 1.1779399999999999E-3 | 2.27764E-3 | 3.9825900000000003E-3 | 7.5578399999999997E-3 | 1.59078E-2 | 2.8375399999999999E-2 | 4.1773999999999999E-2 | 5.5585900000000001E-2 | 7.0088999999999999E-2 | 8.53019E-2 | 0.10122100000000001 | 0.11801499999999999 | 0.135689 | 0.15429399999999999 | 0.173794 | 0.19440199999999999 | 0.216443 | 0.239231 | 0.262573 | 0.28568399999999999 | 0.30929400000000001 | 0.33297700000000002 | 0.35610700000000001 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998
 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005
 | 0 | 0 | 0 | 0 | 0 | 0 | 4.6119e-06 | 1.6519e-05 | 3.2463e-05 | 5.7787e-05 | 0.00011162 | 0.00023875 | 0.00042904 | 0.0006303 | 0.00083481 | 0.0010476 | 0.0012701 | 0.0015024 | 0.0017476 | 0.0020067 | 0.0022805 | 0.0025696 | 0.0028778 | 0.0032109 | 0.0035599 | 0.0039233 | 0.0042899 | 0.0046715 | 0.0050634 | 0.0055008 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 0 | 0 | 3.3295900000000002E-4 | 1.1779399999999999E-3 | 2.27764E-3 | 3.9825900000000003E-3 | 7.5578399999999997E-3 | 1.59078E-2 | 2.8375399999999999E-2 | 4.1773999999999999E-2 | 5.5585900000000001E-2 | 7.0088999999999999E-2 | 8.53019E-2 | 0.10122100000000001 | 0.11801499999999999 | 0.135689 | 0.15429399999999999 | 0.173794 | 0.19440199999999999 | 0.216443 | 0.239231 | 0.262573 | 0.28568399999999999 | 0.30929400000000001 | 0.33297700000000002 | 0.35610700000000001 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998
 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005 | 0.005
 | 0 | 0 | 0 | 0 | 0 | 0 | 4.6119e-06 | 1.6519e-05 | 3.2463e-05 | 5.7787e-05 | 0.00011162 | 0.00023875 | 0.00042904 | 0.0006303 | 0.00083481 | 0.0010476 | 0.0012701 | 0.0015024 | 0.0017476 | 0.0020067 | 0.0022805 | 0.0025696 | 0.0028778 | 0.0032109 | 0.0035599 | 0.0039233 | 0.0042899 | 0.0046715 | 0.0050634 | 0.0055008 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285 | 0.0055285
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 0 | 0 | 3.3295900000000002E-4 | 1.1779399999999999E-3 | 2.27764E-3 | 3.9825900000000003E-3 | 7.5578399999999997E-3 | 1.59078E-2 | 2.8375399999999999E-2 | 4.1773999999999999E-2 | 5.5585900000000001E-2 | 7.0088999999999999E-2 | 8.53019E-2 | 0.10122100000000001 | 0.11801499999999999 | 0.135689 | 0.15429399999999999 | 0.173794 | 0.19440199999999999 | 0.216443 | 0.239231 | 0.262573 | 0.28568399999999999 | 0.30929400000000001 | 0.33297700000000002 | 0.35610700000000001 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998
 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7
 | 1 | 1 | 1 | 1 | 1 | 1 | 1.0007 | 1.0025 | 1.0052 | 1.01 | 1.0198 | 1.0429 | 1.0773 | 1.1145 | 1.1526 | 1.1931 | 1.2354 | 1.2797 | 1.3264 | 1.3755 | 1.4272 | 1.4813 | 1.5384 | 1.5993 | 1.6622 | 1.7265 | 1.7898 | 1.8543 | 1.919 | 1.9818 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 0 | 0 | 3.3295900000000002E-4 | 1.1779399999999999E-3 | 2.27764E-3 | 3.9825900000000003E-3 | 7.5578399999999997E-3 | 1.59078E-2 | 2.8375399999999999E-2 | 4.1773999999999999E-2 | 5.5585900000000001E-2 | 7.0088999999999999E-2 | 8.53019E-2 | 0.10122100000000001 | 0.11801499999999999 | 0.135689 | 0.15429399999999999 | 0.173794 | 0.19440199999999999 | 0.216443 | 0.239231 | 0.262573 | 0.28568399999999999 | 0.30929400000000001 | 0.33297700000000002 | 0.35610700000000001 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998 | 0.35616199999999998
 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7
 | 1 | 1 | 1 | 1 | 1 | 1 | 1.0007 | 1.0025 | 1.0052 | 1.01 | 1.0198 | 1.0429 | 1.0773 | 1.1145 | 1.1526 | 1.1931 | 1.2354 | 1.2797 | 1.3264 | 1.3755 | 1.4272 | 1.4813 | 1.5384 | 1.5993 | 1.6622 | 1.7265 | 1.7898 | 1.8543 | 1.919 | 1.9818 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982 | 1.982
Failure initiates in C-Notch due to coalescence of dilated microvoids

## Slide 16
MLM: Microscopic Damage Mechanisms[Contd.]
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 7.1451000000000001E-4 | 3.1929699999999998E-3 | 7.9347099999999993E-3 | 1.55932E-2 | 2.6228100000000001E-2 | 3.9533800000000001E-2 | 5.4982400000000001E-2 | 7.2180300000000003E-2 | 9.0943599999999999E-2 | 0.11117200000000001 | 0.13273199999999999 | 0.15534999999999999 | 0.179066 | 0.203624 | 0.22862399999999999 | 0.25379000000000002 | 0.27950399999999997 | 0.30521700000000002 | 0.33053300000000002 | 0.354819 | 0.37886900000000001 | 0.401727 | 0.42452000000000001 | 0.44597300000000001 | 0.46659400000000001 | 0.48607899999999998 | 0.50420900000000002 | 0.52132999999999996 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003
 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055
 | 0 | 0 | 0 | 5.6411e-06 | 2.5176e-05 | 6.3848e-05 | 0.00012783 | 0.00021696 | 0.00032865 | 0.00045881 | 0.00060391 | 0.00076172 | 0.00093003 | 0.0011058 | 0.0012855 | 0.0014697 | 0.0016562 | 0.0018438 | 0.0020335 | 0.0022233 | 0.0024197 | 0.0026206 | 0.0028144 | 0.0030041 | 0.0031918 | 0.0033677 | 0.0035351 | 0.0036927 | 0.0038421 | 0.003981 | 0.004108 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 7.1451000000000001E-4 | 3.1929699999999998E-3 | 7.9347099999999993E-3 | 1.55932E-2 | 2.6228100000000001E-2 | 3.9533800000000001E-2 | 5.4982400000000001E-2 | 7.2180300000000003E-2 | 9.0943599999999999E-2 | 0.11117200000000001 | 0.13273199999999999 | 0.15534999999999999 | 0.179066 | 0.203624 | 0.22862399999999999 | 0.25379000000000002 | 0.27950399999999997 | 0.30521700000000002 | 0.33053300000000002 | 0.354819 | 0.37886900000000001 | 0.401727 | 0.42452000000000001 | 0.44597300000000001 | 0.46659400000000001 | 0.48607899999999998 | 0.50420900000000002 | 0.52132999999999996 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003
 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055
 | 0 | 0 | 0 | 5.6411e-06 | 2.5176e-05 | 6.3848e-05 | 0.00012783 | 0.00021696 | 0.00032865 | 0.00045881 | 0.00060391 | 0.00076172 | 0.00093003 | 0.0011058 | 0.0012855 | 0.0014697 | 0.0016562 | 0.0018438 | 0.0020335 | 0.0022233 | 0.0024197 | 0.0026206 | 0.0028144 | 0.0030041 | 0.0031918 | 0.0033677 | 0.0035351 | 0.0036927 | 0.0038421 | 0.003981 | 0.004108 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527 | 0.0041527
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 7.1451000000000001E-4 | 3.1929699999999998E-3 | 7.9347099999999993E-3 | 1.55932E-2 | 2.6228100000000001E-2 | 3.9533800000000001E-2 | 5.4982400000000001E-2 | 7.2180300000000003E-2 | 9.0943599999999999E-2 | 0.11117200000000001 | 0.13273199999999999 | 0.15534999999999999 | 0.179066 | 0.203624 | 0.22862399999999999 | 0.25379000000000002 | 0.27950399999999997 | 0.30521700000000002 | 0.33053300000000002 | 0.354819 | 0.37886900000000001 | 0.401727 | 0.42452000000000001 | 0.44597300000000001 | 0.46659400000000001 | 0.48607899999999998 | 0.50420900000000002 | 0.52132999999999996 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003
 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7
 | 1 | 1 | 1 | 1.0029 | 1.0106 | 1.0252 | 1.0499 | 1.0841 | 1.1274 | 1.1777 | 1.2338 | 1.2949 | 1.3598 | 1.4284 | 1.5018 | 1.5761 | 1.6549 | 1.7349 | 1.8149 | 1.8949 | 1.9749 | 2.0549 | 2.1349 | 2.2149 | 2.2949 | 2.3655 | 2.4341 | 2.5027 | 2.5663 | 2.6234 | 2.6805 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 7.1451000000000001E-4 | 3.1929699999999998E-3 | 7.9347099999999993E-3 | 1.55932E-2 | 2.6228100000000001E-2 | 3.9533800000000001E-2 | 5.4982400000000001E-2 | 7.2180300000000003E-2 | 9.0943599999999999E-2 | 0.11117200000000001 | 0.13273199999999999 | 0.15534999999999999 | 0.179066 | 0.203624 | 0.22862399999999999 | 0.25379000000000002 | 0.27950399999999997 | 0.30521700000000002 | 0.33053300000000002 | 0.354819 | 0.37886900000000001 | 0.401727 | 0.42452000000000001 | 0.44597300000000001 | 0.46659400000000001 | 0.48607899999999998 | 0.50420900000000002 | 0.52132999999999996 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003 | 0.52661400000000003
 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7
 | 1 | 1 | 1 | 1.0029 | 1.0106 | 1.0252 | 1.0499 | 1.0841 | 1.1274 | 1.1777 | 1.2338 | 1.2949 | 1.3598 | 1.4284 | 1.5018 | 1.5761 | 1.6549 | 1.7349 | 1.8149 | 1.8949 | 1.9749 | 2.0549 | 2.1349 | 2.2149 | 2.2949 | 2.3655 | 2.4341 | 2.5027 | 2.5663 | 2.6234 | 2.6805 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007 | 2.7007
Pure Shear – 1
Used for calibrating
Failure initiates in PS-1 due to coalescence of elongated microvoids
U-Notch
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 2.9805400000000002E-4 | 1.5656000000000001E-3 | 3.8471899999999999E-3 | 8.3392099999999997E-3 | 1.56221E-2 | 2.4978E-2 | 3.5881799999999998E-2 | 5.0105400000000001E-2 | 6.8551399999999998E-2 | 9.1757400000000003E-2 | 0.118837 | 0.14774899999999999 | 0.176949 | 0.20610400000000001 | 0.23489599999999999 | 0.26339899999999999 | 0.29141499999999998 | 0.31904300000000002 | 0.346221 | 0.37275599999999998 | 0.39869199999999999 | 0.42404500000000001 | 0.44956499999999999 | 0.47419299999999998 | 0.49771599999999999 | 0.52035900000000002 | 0.54167200000000004 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567
 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055
 | 0 | 0 | 0 | 0 | 2.5585e-06 | 1.4109e-05 | 3.4888e-05 | 7.7061e-05 | 0.00014839 | 0.00023944 | 0.00034251 | 0.00047394 | 0.00064242 | 0.00085298 | 0.001097 | 0.0013548 | 0.0016132 | 0.0018685 | 0.0021192 | 0.0023661 | 0.0026077 | 0.0028452 | 0.0030765 | 0.0033038 | 0.0035229 | 0.0037352 | 0.0039488 | 0.0041552 | 0.0043505 | 0.0045409 | 0.0047164 | 0.0055306
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 2.9805400000000002E-4 | 1.5656000000000001E-3 | 3.8471899999999999E-3 | 8.3392099999999997E-3 | 1.56221E-2 | 2.4978E-2 | 3.5881799999999998E-2 | 5.0105400000000001E-2 | 6.8551399999999998E-2 | 9.1757400000000003E-2 | 0.118837 | 0.14774899999999999 | 0.176949 | 0.20610400000000001 | 0.23489599999999999 | 0.26339899999999999 | 0.29141499999999998 | 0.31904300000000002 | 0.346221 | 0.37275599999999998 | 0.39869199999999999 | 0.42404500000000001 | 0.44956499999999999 | 0.47419299999999998 | 0.49771599999999999 | 0.52035900000000002 | 0.54167200000000004 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567
 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055
 | 0 | 0 | 0 | 0 | 2.5585e-06 | 1.4109e-05 | 3.4888e-05 | 7.7061e-05 | 0.00014839 | 0.00023944 | 0.00034251 | 0.00047394 | 0.00064242 | 0.00085298 | 0.001097 | 0.0013548 | 0.0016132 | 0.0018685 | 0.0021192 | 0.0023661 | 0.0026077 | 0.0028452 | 0.0030765 | 0.0033038 | 0.0035229 | 0.0037352 | 0.0039488 | 0.0041552 | 0.0043505 | 0.0045409 | 0.0047164 | 0.0055306
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 2.9805400000000002E-4 | 1.5656000000000001E-3 | 3.8471899999999999E-3 | 8.3392099999999997E-3 | 1.56221E-2 | 2.4978E-2 | 3.5881799999999998E-2 | 5.0105400000000001E-2 | 6.8551399999999998E-2 | 9.1757400000000003E-2 | 0.118837 | 0.14774899999999999 | 0.176949 | 0.20610400000000001 | 0.23489599999999999 | 0.26339899999999999 | 0.29141499999999998 | 0.31904300000000002 | 0.346221 | 0.37275599999999998 | 0.39869199999999999 | 0.42404500000000001 | 0.44956499999999999 | 0.47419299999999998 | 0.49771599999999999 | 0.52035900000000002 | 0.54167200000000004 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567
 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7
 | 1 | 1 | 1 | 1 | 1.001 | 1.0045 | 1.0116 | 1.0251 | 1.047 | 1.0752 | 1.1082 | 1.1515 | 1.208 | 1.2788 | 1.3617 | 1.4501 | 1.5396 | 1.6293 | 1.7166 | 1.803 | 1.8894 | 1.9744 | 2.0576 | 2.1408 | 2.2208 | 2.2976 | 2.3768 | 2.4501 | 2.5235 | 2.5915 | 2.6581 | 2.7006
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 2.9805400000000002E-4 | 1.5656000000000001E-3 | 3.8471899999999999E-3 | 8.3392099999999997E-3 | 1.56221E-2 | 2.4978E-2 | 3.5881799999999998E-2 | 5.0105400000000001E-2 | 6.8551399999999998E-2 | 9.1757400000000003E-2 | 0.118837 | 0.14774899999999999 | 0.176949 | 0.20610400000000001 | 0.23489599999999999 | 0.26339899999999999 | 0.29141499999999998 | 0.31904300000000002 | 0.346221 | 0.37275599999999998 | 0.39869199999999999 | 0.42404500000000001 | 0.44956499999999999 | 0.47419299999999998 | 0.49771599999999999 | 0.52035900000000002 | 0.54167200000000004 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567
 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7
 | 1 | 1 | 1 | 1 | 1.001 | 1.0045 | 1.0116 | 1.0251 | 1.047 | 1.0752 | 1.1082 | 1.1515 | 1.208 | 1.2788 | 1.3617 | 1.4501 | 1.5396 | 1.6293 | 1.7166 | 1.803 | 1.8894 | 1.9744 | 2.0576 | 2.1408 | 2.2208 | 2.2976 | 2.3768 | 2.4501 | 2.5235 | 2.5915 | 2.6581 | 2.7006
Failure initiates in U-Notch due to coalescence of dilated and elongated microvoids

## Slide 17
MLM: Microscopic Damage Mechanisms[Contd.]
Shear Tension
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 2.9805400000000002E-4 | 1.5656000000000001E-3 | 3.8471899999999999E-3 | 8.3392099999999997E-3 | 1.56221E-2 | 2.4978E-2 | 3.5881799999999998E-2 | 5.0105400000000001E-2 | 6.8551399999999998E-2 | 9.1757400000000003E-2 | 0.118837 | 0.14774899999999999 | 0.176949 | 0.20610400000000001 | 0.23489599999999999 | 0.26339899999999999 | 0.29141499999999998 | 0.31904300000000002 | 0.346221 | 0.37275599999999998 | 0.39869199999999999 | 0.42404500000000001 | 0.44956499999999999 | 0.47419299999999998 | 0.49771599999999999 | 0.52035900000000002 | 0.54167200000000004 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567
 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055
 | 0 | 0 | 0 | 0 | 1.6096e-06 | 1.3706e-05 | 3.6224e-05 | 7.7769e-05 | 0.00015553 | 0.00027696 | 0.00042441 | 0.00058509 | 0.0007546 | 0.00093047 | 0.0011109 | 0.0012945 | 0.0014803 | 0.001668 | 0.0018567 | 0.0020453 | 0.0022328 | 0.0024203 | 0.0026078 | 0.0027953 | 0.0029828 | 0.0031656 | 0.0033468 | 0.0035281 | 0.0037091 | 0.0038813 | 0.0040555 | 0.0042291 | 0.0043917 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 2.9805400000000002E-4 | 1.5656000000000001E-3 | 3.8471899999999999E-3 | 8.3392099999999997E-3 | 1.56221E-2 | 2.4978E-2 | 3.5881799999999998E-2 | 5.0105400000000001E-2 | 6.8551399999999998E-2 | 9.1757400000000003E-2 | 0.118837 | 0.14774899999999999 | 0.176949 | 0.20610400000000001 | 0.23489599999999999 | 0.26339899999999999 | 0.29141499999999998 | 0.31904300000000002 | 0.346221 | 0.37275599999999998 | 0.39869199999999999 | 0.42404500000000001 | 0.44956499999999999 | 0.47419299999999998 | 0.49771599999999999 | 0.52035900000000002 | 0.54167200000000004 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567
 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055
 | 0 | 0 | 0 | 0 | 1.6096e-06 | 1.3706e-05 | 3.6224e-05 | 7.7769e-05 | 0.00015553 | 0.00027696 | 0.00042441 | 0.00058509 | 0.0007546 | 0.00093047 | 0.0011109 | 0.0012945 | 0.0014803 | 0.001668 | 0.0018567 | 0.0020453 | 0.0022328 | 0.0024203 | 0.0026078 | 0.0027953 | 0.0029828 | 0.0031656 | 0.0033468 | 0.0035281 | 0.0037091 | 0.0038813 | 0.0040555 | 0.0042291 | 0.0043917 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268 | 0.0054268
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 2.9805400000000002E-4 | 1.5656000000000001E-3 | 3.8471899999999999E-3 | 8.3392099999999997E-3 | 1.56221E-2 | 2.4978E-2 | 3.5881799999999998E-2 | 5.0105400000000001E-2 | 6.8551399999999998E-2 | 9.1757400000000003E-2 | 0.118837 | 0.14774899999999999 | 0.176949 | 0.20610400000000001 | 0.23489599999999999 | 0.26339899999999999 | 0.29141499999999998 | 0.31904300000000002 | 0.346221 | 0.37275599999999998 | 0.39869199999999999 | 0.42404500000000001 | 0.44956499999999999 | 0.47419299999999998 | 0.49771599999999999 | 0.52035900000000002 | 0.54167200000000004 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567
 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7
 | 1 | 1 | 1 | 1 | 1.0005 | 1.0051 | 1.0134 | 1.0288 | 1.0562 | 1.0979 | 1.1488 | 1.2053 | 1.2662 | 1.3302 | 1.397 | 1.4653 | 1.5356 | 1.6061 | 1.677 | 1.7486 | 1.8204 | 1.8911 | 1.9615 | 2.0319 | 2.1023 | 2.1727 | 2.2431 | 2.3135 | 2.3839 | 2.4501 | 2.5141 | 2.5781 | 2.6421 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 2.9805400000000002E-4 | 1.5656000000000001E-3 | 3.8471899999999999E-3 | 8.3392099999999997E-3 | 1.56221E-2 | 2.4978E-2 | 3.5881799999999998E-2 | 5.0105400000000001E-2 | 6.8551399999999998E-2 | 9.1757400000000003E-2 | 0.118837 | 0.14774899999999999 | 0.176949 | 0.20610400000000001 | 0.23489599999999999 | 0.26339899999999999 | 0.29141499999999998 | 0.31904300000000002 | 0.346221 | 0.37275599999999998 | 0.39869199999999999 | 0.42404500000000001 | 0.44956499999999999 | 0.47419299999999998 | 0.49771599999999999 | 0.52035900000000002 | 0.54167200000000004 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567
 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7
 | 1 | 1 | 1 | 1 | 1.0005 | 1.0051 | 1.0134 | 1.0288 | 1.0562 | 1.0979 | 1.1488 | 1.2053 | 1.2662 | 1.3302 | 1.397 | 1.4653 | 1.5356 | 1.6061 | 1.677 | 1.7486 | 1.8204 | 1.8911 | 1.9615 | 2.0319 | 2.1023 | 2.1727 | 2.2431 | 2.3135 | 2.3839 | 2.4501 | 2.5141 | 2.5781 | 2.6421 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008 | 2.7008
Failure initiates in U-Notch due to coalescence of dilated and elongated microvoids
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 2.9805400000000002E-4 | 1.5656000000000001E-3 | 3.8471899999999999E-3 | 8.3392099999999997E-3 | 1.56221E-2 | 2.4978E-2 | 3.5881799999999998E-2 | 5.0105400000000001E-2 | 6.8551399999999998E-2 | 9.1757400000000003E-2 | 0.118837 | 0.14774899999999999 | 0.176949 | 0.20610400000000001 | 0.23489599999999999 | 0.26339899999999999 | 0.29141499999999998 | 0.31904300000000002 | 0.346221 | 0.37275599999999998 | 0.39869199999999999 | 0.42404500000000001 | 0.44956499999999999 | 0.47419299999999998 | 0.49771599999999999 | 0.52035900000000002 | 0.54167200000000004 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567
 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055 | 0.0055
 | 0 | 0 | 0 | 7.4657e-06 | 3.2204e-05 | 8.1601e-05 | 0.00015505 | 0.00024441 | 0.00035323 | 0.00048685 | 0.00064657 | 0.00083154 | 0.0010403 | 0.0012689 | 0.0015155 | 0.0017808 | 0.0020628 | 0.0023578 | 0.0026638 | 0.0029763 | 0.0032905 | 0.003603 | 0.0039113 | 0.0042146 | 0.0045111 | 0.0047969 | 0.0050628 | 0.0053093 | 0.0060338 | 0.0060338 | 0.0060338 | 0.0060338 | 0.0060338 | 0.0060338 | 0.0060338 | 0.0060338 | 0.0060338 | 0.0060338 | 0.0060338 | 0.0060338 | 0.0060338
Pure Shear - 2
Chart: Effective Plastic Strain
| 0 | 0 | 0 | 0 | 2.9805400000000002E-4 | 1.5656000000000001E-3 | 3.8471899999999999E-3 | 8.3392099999999997E-3 | 1.56221E-2 | 2.4978E-2 | 3.5881799999999998E-2 | 5.0105400000000001E-2 | 6.8551399999999998E-2 | 9.1757400000000003E-2 | 0.118837 | 0.14774899999999999 | 0.176949 | 0.20610400000000001 | 0.23489599999999999 | 0.26339899999999999 | 0.29141499999999998 | 0.31904300000000002 | 0.346221 | 0.37275599999999998 | 0.39869199999999999 | 0.42404500000000001 | 0.44956499999999999 | 0.47419299999999998 | 0.49771599999999999 | 0.52035900000000002 | 0.54167200000000004 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567 | 0.55567
 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7 | 2.7
 | 1 | 1 | 1 | 1.0025 | 1.0114 | 1.0285 | 1.054 | 1.0854 | 1.1221 | 1.1652 | 1.2146 | 1.2701 | 1.3303 | 1.3941 | 1.4605 | 1.5298 | 1.5998 | 1.67 | 1.7401 | 1.8101 | 1.8792 | 1.9459 | 2.0099 | 2.0699 | 2.127 | 2.1804 | 2.2273 | 2.2692 | 2.3013 | 2.3013 | 2.3013 | 2.3013 | 2.3013 | 2.3013 | 2.3013 | 2.3013 | 2.3013 | 2.3013 | 2.3013 | 2.3013 | 2.3013
Failure initiates in PS-1 due to coalescence of elongated microvoids

## Slide 18
MLM: Specimen Fracture Locus
Chart: Average Initial Triaxiality
| 0.10100000000000001 | 8.9599999999999999E-2 | 0.35499999999999998 | 0.46600000000000003 | 0.53 | 0.56499999999999995
 | 0.14821 | 0.22768 | 0.10804 | 0.1 | 0.080357
 | 0.15357 | 0.20982 | 0.086607 | 0.099107 | 0.078571
Relative displacement change in length; gage length (11.2 mm)
Average initial triaxiality – average triaxiality in the critical cross-section A-A (least cross-sectional area shown in the schematics – left side)
Experiment
MLM prediction
Experimental result match with MLM prediction
11.2 mm
11.2 mm
A
A
A
A
Critical cross-sections
Gage lengths