## Slide 1
Ferrite & Martensite: Rate Dependent Plasticity
Additive decomposition of strain rate tensor
- elastic strain rate tensor
- plastic strain rate tensor
Evolution of plastic strain rate
- hardening strength
– strain rate parameters
Isotropic hardening law
, ,, and – hardening parameters

## Slide 2
Ferrite & Martensite: Rate Dependent Plasticity[Contd.]
Phase | (Mpa) | (Mpa) | (Mpa) |  |  |  | 
Martensite | 780 | 350 | 525 | 370 | 1.0 | 0.21 | 0.01
Ferrite | 540 | 1500 | 175 | 330 | 1.0 | 0.21 | 0.01
Phase |  |  |  |  |  |  | 
Martensite | 780 | 350 | 525 | 370 | 1.0 | 0.21 | 0.01
Ferrite | 540 | 1500 | 175 | 330 | 1.0 | 0.21 | 0.01
Chart: Strain

Chart: Strain


Ferrite
Martensite
Crystal plasticity
Isotropic plasticity
Isotropic plasticity curves matched well with crystal plasticity predictions

## Slide 3
Retained Austenite
Features of retained austenite model:
accounts for phase transformation strain
accounts for dilation due to phase transformation
Additive decomposition of strain rate tensor
- martensitic transformation strain rate tensor
Composite model properties
, - yield strength of austenite and martensite phases
, - isotropic hardening properties of austenite
, - isotropic hardening properties of martensite
– martensite volume fraction
Accounts for the composite effect of
retained austenite and transformed martensite

## Slide 4
Retained Austenite[Contd.]
, - transformation constants; - dilatational constant
Evolution of transformation induced plasticity strain tensor[1]
where the evolution of the martensite volume is given as
Both stress and strains can influence evolution of martensite volume. However, this influence is limited by choosing and
- critical effective strain; - threshold effective strain
- threshold effective stress
[1] Mahnken, R., A. Schneidt, et al. (2009). International Journal of Plasticity 25(2): 183-204.

## Slide 5
Phase | (Mpa) | (Mpa) | (Mpa) |  |  |  |  |  | 
RA | 400 | 5200 | 6800 | 450 | 600 | 4.2 | 1.05 | 0.01 | 0.21
Phase |  |  |  |  |  |  |  |  | 
RA | 400 | 5200 | 6800 | 450 | 600 | 4.2 | 1.05 | 0.01 | 0.21
Retained Austenite[Contd.]
Hardening properties
(1/Mpa) | (1/Mpa2) |  |  | (Mpa)
400 | 5200 | 6800 | 450 | 600
400 | 5200 | 6800 | 450 | 600
Phase transformation properties
Chart: Strain
Chart: Strain
Crystal plasticity
Trans. Model
The isotropic martensitic transformation model accurately reproduces the crystal plasticity predictions accurately

## Slide 6
Q&P 980 Steel – Isotropic Model
Ferrite – 50%
Martensite – 42%
RA – 8%
Chart: Strain
Chart: Strain
 | 0 | 0.094 | 0.233 | 0.39 | 0.562 | 0.714 | 0.734
Crystal plasticity
Trans. Model